## Slide 1
Hideo Aoki
Dept Physics, Univ Tokyo, Japan
&
AIST, Tsukuba, Japan
Int. Workshop“CORPES 2022”
online, 14 July 2022
Engineering superconducting and topological systems
in and out of equilibrium

## Slide 2
Superconductivity Topological
(from repulsion)
Incipient-band SC
* a new cuprate
* flat bands
Floquet topological insulator
Non-equil
Equilibrium
Plan of the talk
* Floquet topological d + id SC
Incipient-band SC
Floquet-engineered SC

## Slide 3
An incipient band can favour SC
even for a cuprate theoretically.
Good cuprates are one-band
--- Q: Is this always the case ?

## Slide 4
High Tc in single-layer Ba2CuO3+d d  0.2 (≡ Ba2CuO4-y y = 1-d  0.8)
a = 3.76 Å
c = 12.57 Å
Cu-O plane
a = 3.4954 Å
b = 3.9057 Å
c = 12.68 Å
La2CuO4
a = 3.78 Å
c = 13.2 Å
CuO-chain
Ba2CuO3
≡ Ba2CuO4-y
Ba2CuO3+d
Ba2CuO4
oxygen depletion
oxygen depletion
octahedron
fully occupied apical O
In-plane O vacancies
(Li et al, PNAS 2019)
Various theoretical proposals for the el structure
(Maier, …, Scalapino, PRB 2019; Liu et al, PRMat 2019, …)
● Heavily hole-doped (p = 2d  0.4/Cu)
● Heavily (40%) O-deficient Cu-O plane
Ba22+Cu2+pO3+d, d  0.2
Ba2CuO2(1-y/2)O2
inplane
apical
* Experimentally, a tetragonal structure suggested

## Slide 5
Planar Apex
(Ba2CuO3)4 = Ba8Cu4O12 = (Cu4O4) (Ba2O2)4
O (apex)
Cu
O (in-plane)
Mother (undoped) compound: Ba2CuO3
(Yamazaki et al, PRR 2020)
Bird's eye view
orbital 1(dx2-y2)
orbital 2(dz2)
intra-orbital extended s inter-o d
D11 D22 D12
gap function(FLEX)

## Slide 6
intra-orbital s-wave;
inter-orbital d-wave
Tc dome
(Yamazaki et al, PRR 2020)
Usual one-band d-wave
comes from an
“incipient band”
DE

## Slide 7
Incipient (close to, but away from E F) bands
as in FeSe (Qian et al, PRL 2011; …)
+
+
-
incipient s
E F
+
+
Originally, the concept of
"incipient bands" introduced by
Kuroki et al, PRB 2005
The notion works even in the strong-U regime:
(DCA: Maier, …, Scalapino, PRB 2019;
Karakuzu, ..., Maier, PRB 2021;
VMC: Kato & Kuroki, PRR 2020)
(ARPES: Rinott et al, Sci Adv 2017)

## Slide 8
SC in incipient flat-bands/flat portions
2-band
1-band
EF
* Higher Tc in both cases
EF
incipient
incipient

## Slide 9
Repulsive Hubbard model on diamond chain
(a simplest possible 1D flat-b)
(Kobayashi et al, PRB 2016)
non-orthogonalisable Wannier

## Slide 10
Phase diagram
1/3
1
TI
band filling
1/2
0
2/3
Flat-b F
Incipient flat band
SC adjacent to a
topological phase
EF
(DMRG; Kobayashi et al, PRB 2016)

## Slide 11
Variouos flat-band models
(Matsumoto, Ogura & Kuroki, PRB 2018; JPSJ 2020)
What determines the dip-width ?
Tc ~ 0.08t
(cf. cuprates' Tc ~ 0.03t)
EF
m - Eflat
Spin susceptibility (w)
higher-E region:
pair enhancing
low-E region:
pair breaking
✔ Low-E spin fluctuations  degrade SC (m shouldn't be too close to E flat)
[For ordinary d- and s-wave SCs, this has been shown by
Millis-Sachdev-Varma(PRB 1988)  present case is its s± version]

## Slide 12
2-band vs 1-band flat-band SC
2-band
1-band
EF

## Slide 13
Partially-flat band
(Sayyad et al, PRB 2020)
cspin
Green's function
t
t'
t'~ -0.5t (a kind of frustration)

## Slide 14
t-t', singlet
Eliashberg
(Sayyad et al, PRB 2020)
Tc dome
k-space
Method:
FLEX+DMFT,
DQMC
real-space
unusually extended pair
t-t' model

## Slide 15
A hint: t-t'-t"-U (≫t) model on a square lattice
(Delannoy, ..., Tremblay, PRB 2009)
Half-filled t-U (≫ t) model (1/U) expansion up to O(1/U3)

 inclusion of t', t" makes it even more complicated
My guess:
Ring-exchange interactions tend
to be enhanced in flat bands
Why frustrated t-t' model?
Heisenberg AF
4-site ring exchanges

## Slide 16
Dimensionality-dependence:
Usually, SC from el-el repulsion works much better in 2D than in 3D
(Arita et al, 1999;
Monthoux & Lonzarich, 1999)
Cu, Ru compounds Co compound Hf compound Ce compound Fe compound
>
Orange: Large spin-fluct mediated
pairing int.
Qx
ky
+
+
-
-
Qz
Qx
ky
kz
+
+
+
+
-
-
-
-
q2D 3D
AF
AF

## Slide 17
Flat-band SC has totally different dim-dep
Narrow-wide band system(Kuroki et al, PRB 2005)
spin susc featureless
s pairing
over entire Bz
+
-
dispersive band
flat band
1D
Qx
Qy
Qz
Specialty of the flat-band SC
(beyond the nesting physics):
→ 3D as good as 2D
(evades Arita's & Lonzarich's theorem)
3D
Partially-flat band(Sayyad et al, PRB 2020)
2D
cs broad in k gap f mom distr

## Slide 18
vgroup = 0 at a point: van Hove sing.  topological SC (d+id, etc)
+ i
vgroup = 0 in finite areas in flat bands
Honeycomb with EF ~ v Hove TBG (Liu et al, PRL 2018) kagome (Wu et al, PRL 2021)
(Nandkishore et al, nat phy 2012)
Square Triangular
Electronic nematicity
 enhances SC
(Sayyad et al, arXiv:2110.14268)
d+id
d+id

## Slide 19
● Usually, no, or only small (2nd-order) effects
(e.g., Kitatani, Tsuji & Aoki, PRB 2017)
● In triangular lattice
* frustration
 enhances nematicity
 concomitantly enhances SC
(almost doubles Tc, a 1st-order effect)
(Sayyad et al, arXiv:2110.14268, now
published in J Phys Condensed Matter 2023)
A question: Can electronic nematicity enhance SC?
t' = 0.15

## Slide 20
(FLEX+DMFT, Sayyad et al, JPCM 2023)
n = 0.9 n = 1.0 n = 1.1
Momentum distr
cspin
Green's function
Nematic (C6 symmetry  C2)
Spectral f A(k, w)

## Slide 21
(Sayyad et al, JPCM 2023)
(Triangular) t'=0.15
Eliashberg l
Nematicity forbidden
Nematicity allowed
t-t', singlet
(Sayyad et al, PRB 2020)
(Square) t'=0.5
Nematicity x

## Slide 22
(Sayyad et al, JPCM 2023)
n =0.9 n = 1.0 n = 1.1
dx2-y2
in C6 point-group irred rep
(y2 in C2 (nematic phase) point-gr)
Gap function
Pairing interaction, hence l, significantly enhanced
Cf. tetragonal lattice,
where 1st-order effect of nematicity
on l identically vanishes

## Slide 23
Superconductivity Topological
(from repulsion)
Incipient-band SC
* a new cuprate
* flat bands
Floquet topological insulator
Non-equil
Equilibrium
Plan of the talk

## Slide 24
Floquet topological insulator
(Oka & Aoki, PRB 2009)
B = 0
topological gap opens
dynamically
Chern density
Hall current
Experimental detection of FTI in graphene
(McIver et al, 2020)
Quantum anomalous Hall effect (QHE in B=0)

## Slide 25
(MIT)
First detection of FTI: surface of 3D TI
(see also: Mahmood, …,
Gedik, nature phys 2016)

## Slide 26
Superconductivity Topological
(from repulsion)
Incipient-band SC
* a new cuprate
* flat bands
Floquet topological insulator
Non-equil
Equilibrium
Plan of the talk
* Floquet topological d + id SC
(in a t-t' model)

## Slide 27
T-broken SC  usually from coexisting pairing symmetries
in equilibrium
- eg, proposed for iron-based SCs
Lee, Zhang & Wu, PRL 2009 for "1111";
Fernandes & Millis, PRL 2013 for "122"
Ahn et al, PRB 2014 for LiFeAs
s+-(A) s+-(B)
s+- d
+
+
-
-
T
T
An entirely different (dynamical) way ― Floquet

## Slide 28
(Kitamura & Aoki, Comm Phys 2022)
graphene
Mott insulator
d-wave SC
FTI
chiral spin states
d+id wave SC
Dirac (one-body)
Strongly-correlated systems
(Oka & Aoki, PRB 2009)
(Kitamura, Oka & Aoki, PRB 2017;
Claassen et al, nat comm 2017)
real space
k space
This is not so simple,
because laser doesn't couple with gap function

## Slide 29
Go to strong-coupling regime
to realise d-wave SC + CPL  "Floquet topological (dx2-y2 + idxy)SC"
(Kitamura & Aoki, Comm Phys 2022)
t
t'
Repulsive Hubbard model + CPL
on a square lattice
t << U  * No CPL  t-J model [strong-coupl. (Schrieffer-Wolff)expansion]
* Under CPL  Floquet extension (for t << w < U )
Floquet renormalised hopping
photon-induced chiral
spin coupling
photon-induced correlated hopping
photon-modified kinetic exchange
~

## Slide 30
t
honeycomb
this is why graphene accommodates FTI
+ =
Haldane's model
One-body problem
square
cancellation
no cancellation
Strongly-correlated case
square lattice already
accommodates topology
(Kitamura & Aoki, Comm Phys 2022)

## Slide 31
Floquet Hamiltonian in Bogoliubov-de Gennes form
t
t'
acquires a dxy component  sin(kx) sin(ky) involving
chiral spin-coupling
d: doping, g=2/(1+ d)
 dx2-y2 + idxy
two-step correlated hopping
(Mean-field analysis for H Floquet with Gutzwiller projection,
Kitamura & Aoki, Comm Phys 2022)

## Slide 32
Two-step correlated hopping
Chiral spin-coupling
laser field intensity
laser frequency
Series of "w-U" resonances
(t' = -0.2t, U = 12t, d = 0.2)
(Kitamura & Aoki, Comm Phys 2022)

## Slide 33
Gap function
topological gap
amplitude phase
=
(Kitamura & Aoki, Comm Phys 2022)

## Slide 34
Photon-induced interactions behave as:
For an optimal E , idxy component = i 0.3t sin(kx) sin(ky),
☺ remarkably ≈ dx2-y2 = 0.7t [cos(kx) -cos(ky)]  large topological gap
two-step correlated hopping
g: expression in terms of J2(Ea/w)×(w-U resonance factor),
peaked around E ~ 2w/a as a f of E, diverges for w  0 or U/2
☺ g is significant even in low-w regime, which helps required E  w
Taylor-expand in E  g ~ t t' E4 × (function of w, U )
Jc: expression in terms of Jm(Ea/w)'s×(w-U resonance factor),
☺ diverges for w  U
Taylor-expand in E  Jc ~ (t t' )2 E4 × (function of w, U )
J: strongly-enhanced AF when slightly red-detuned from U/2 or U
t-t' model needed
chiral spin-coupling
kinetic exchange (photon-assisted)
(Kitamura & Aoki, Comm Phys 2022)

## Slide 35
"Tc dome" against laser intensity for the (d + id) SC
|D|
Im D
temperature
laser field intensity
CPL-incuded SC
---:
T eff in Floquet Hamlitonian
topological
(Kitamura & Aoki, Comm Phys 2022)

## Slide 36
Quench dynamics
confirms this
|D|
Im D
Switch on
the laser
|D|
Im D
Switch on
the laser
nonequilibrium-induced SC
time scale for damped osc ~ 1/(gap f)
oscillation = Higgs A2g mode
oscillation = Higgs A2g mode
(Kitamura & Aoki, Comm Phys 2022)

## Slide 37
Experiment + theory on Bi2212
Higgs modes in a HTC cuprate
The present topological SC intimately related to Higgs mode excitations
 an interesting possibility: topological SC enhanced by
resonantly exciting the Higgs

## Slide 38
＊Usually, materials design (elements/crys str)
Design for correlated systems
＊Design on t-axis
(in other words, design in 4D with the 4th dim = time)

## Slide 39
THz (pulse)
(Hirori et al; Watanabe et al)
Photo-induced insulator-metal tr
(Wall et al, Nat. Phys. 2010)
We can have intense enough laser for topological phases
Floquet topological SC
(present proposal)for
typical cuprates with
t ~ 0.4 eV, w ~ U, a ~ 3 Å
Required intensity reduced by
(i) going to honeycomb/kagome,
(ii) lower w
FTI in graphene
(McIver et al, nat phys 2020)
Laser frequency w (eV)
Laser field E (eV/m)
Required for FTI with
topological gap ~ 0.1eV

## Slide 40
Superconductivity / Topological
✔ Incipient-band SC
* Effective in flat bands
* Possibly work even in a cuprate
* Nematicity can enhance SC
Non-equil
Equilibrium
✔ Topological d + id SC
* realisable in a t-t' model by CPL with realistic intensities
These indeed harbour unique opportunities
giving a prospect of quantum phases
Summary: take-home messages
Future works:
Competition with other phases

## Slide 41
Sota Kitamura Univ Tokyo
Sharareh Sayyad Univ Tokyo, now at Erlangen
Abolhassan Vaezi, Edwin Huang Stanford
Mohammad-Sadegh Vaezi Pasargad Institute
Zohar Nussinov Washington Univ
Motoharu Kitatani TU Wien, now at Riken
Kimihiro Yamazaki, Masayuki Ochi, Daisuke Ogura, Kazuhiko Kuroki Osaka Univ
Hiroshi Eisaki AIST
Shinichi Uchida AIST/CAS